## Slide 1
Aircraft Materials
Processing – Microstructure – Property Relations
Case Study
(by Dr S Gowthaman)
Objectives:
To present overview of materials used in aircraft structures.
To highlight the influence of processing – microstructure – property relations in certain aircraft material (polymer composites).

## Slide 6
The properties / performance of materials are linked to:
chemical composition
processing path
microstructure of the material
Composition - Processing - Microstructure - Property Relations

## Slide 7
To select a material for a particular component, the designer must have an intimate knowledge of what properties are required – Designers should be aware of various materials available and their mechanical, thermal, electronic, and other properties.
Example mechanical properties:
Strength
Tensile strength (ultimate strength)
Yield strength
Compressive strength
Hardness
Toughness
Notch toughness
Fracture toughness
Ductility
Total elongation
Reduction in area
Fatigue resistance
Example other properties:
Formability
Drawability
Stretchability
Bendability
Wear resistance
Abrasion resistance
Galling resistance
Sliding wear resistance
Composition - Processing - Microstructure - Property Relations

## Slide 8
In the selection process, what is required for one application may be totally inappropriate for another application.
Example: Steel beams for a railway bridge
Certain Requirements:
Strength to withstand the loads.
Fracture toughness to resist crack growth
Weldability with other steel beams (need low carbon)
Chosen material: HSLA steel has a ferrite-pearlite microstructure and is microalloyed with vanadium and/or niobium for strengthening.
(Microalloying is a term used to describe the process of using small additions of carbonitride forming elements--titanium, vanadium, and niobium--to strengthen steels by grain refinement and precipitation hardening.)
Example: Steel rails
Certain Requirements:
High strength
Wear resistance
Chosen material: Modern rail steels consist of a fully pearlitic microstructure with a fine pearlite interlamellar spacing. Pearlite is unique because it is a lamellar composite consisting of 88% soft, ductile ferrite and 12% hard, brittle cementite (Fe3C). The hard cementite plates provide excellent wear resistance, especially when embedded in soft ferrite. Pearlitic steels have high strength and are fully adequate to support heavy axle loads of modern locomotives and freight cars.
Ferrite-pearlite microstructure
Fully pearlite microstructure
So, the requirements for these applications are different and hence the information on processing – microstructure – property relations help designers.
Composition - Processing - Microstructure - Property Relations

## Slide 9
In this case study, we will discuss
Composition - Processing - Microstructure - Property relations in a certain aircraft material which will be useful for designing of aircraft structures…..
Material to be discussed – Polymer composites (PMCs)

## Slide 10
Fiber reinforcements
Inorganic
Glass
Boron/tungsten wire
Silicon carbide
Organic
Aramid (Kevlar)
Carbon
Graphite
Polymer Matrix Composites
Possible Compositions
Metal
Stainless steel alloy
Aluminum alloy
Titanium alloy
Carbon
Carbonized resin
CVD carbon or graphite
Carbon powder
Fillers
Powder
Silica
Carbon
Microballoon
Phenolic
Carbon
Glass
Possible Reinforcement Forms
Matrix materials
Thermoplastic
Polyester
Polyamide
Polysulfone
Thermoset
Epoxy
Phenolic
Polyester
Polyimide
Bismaleimide
Pitch
Compositions influence the type of processing and resulting microstructure / properties……..

## Slide 11
Mechanical properties and service temperatures for selected reinforcement fibers
Inorganic fibers: glass (maximum temperature 970 °C) and aramid (maximum temperature 500 °C).
Organic fibers: carbon (maximum temperature 2500 °C) and graphite (maximum temperature 3000 °C
Polymer Matrix Composites
Compositions influence the type of processing and resulting microstructure / properties……..
Density
Strength
Modulus

## Slide 12
Polymer Matrix Composites
Compositions influence the type of processing and resulting microstructure and properties……..
Density
Strength
Modulus
Mechanical properties and service temperatures for selected matrix resins
Thermoplastics: polyester (unfilled; maximum temperature 140 °C), polyamide (nylon 6/6, unfilled; maximum temperature 130 °C), and polysulfone (standard; maximum temperature 160 °C).
Thermosets: epoxy (unfilled; maximum temperature 260 °C), phenolic (unfilled; maximum temperature 230°C) and polyimide (unfilled; maximum temperature 370 °C)

## Slide 13
Forms of composition influences microstructure and properties……Effect of fiber orientation on the strength of carbon-fiber/epoxy composites is shown in the Figure.
Polymer Matrix Composites

## Slide 14
Type of processing influences the microstructure and properties – Glass / epoxy composites
Polymer Matrix Composites
Hand lay-up
Vacuum bagging
Vacuum infusion of resin
More air bubbles
Less air bubbles
No air bubbles
Microstructure
Microstructure
Microstructure
Properties

## Slide 15
Problem - Structural failure
Property needed - Strength, stiffness, toughness
Problem - Icing
Property needed - Electrical & thermal conductivity
Problem - Lightning
Property needed - Electrical conductivity
Problem - Structural health monitoring
Property needed - Electrical conductivity, self healing
Materials Needs for Some Aircraft Applications
We will see some materials solutions for these from composition – processing – microstructure – property perspective…
Still there are needs of new materials for many challenges in aircraft structures….some examples are shown below.

## Slide 16
resin impregnation
VARTM
nanoresin
Vacuum pump
fabric
Hand mix epoxy + CNT
Process in three roll mill
Materials Needs for Aircraft Applications (Mechanical Properties)
Composition: CNT + Epoxy + Carbon fiber composite
Processing
Microstructure
Non uniform mixing of CNT
Processing of composites
Use nanoresin now to make composite
Resulting strength, modulus of composites is not good (because of non uniform mixing of CNTs)
Property
Problem - Structural failure
Property needed - Strength, stiffness, toughness

## Slide 17
resin impregnation
VARTM
resin
Vacuum pump
CNT coated fabric
Composition: CNT + PC + Carbon fiber composite
Processing
Microstructure
Electrophoretic deposition
Uniform coating of CNT on fabrics
Problem - Structural failure
Property needed - Strength, stiffness, toughness
Processing of composites
Use CNT coated fabric now to make composite
Property
Resulting strength, modulus of composites is good (because uniform deposition of CNTs)
(Note - Figure shows with some chemical treatment along with CNT coatings)
Materials Needs for Aircraft Applications (Mechanical Properties)

## Slide 18
Composition: Nylon nanofiber + Epoxy + Carbon fiber composite
Processing
Microstructure
Processing of composites
Electrospinning
Nylon nanofibers
resin impregnation
VARTM
resin
Vacuum pump
Nylon coated fabric
Processing of composites
Use Nylon coated fabric now to make composite
Fabric stacking
Problem - Structural failure
Property needed - Strength, stiffness, toughness
Fracture toughness improved by 150%
(nanofiber bridging, pull out are mechanisms)
Property
Materials Needs for Aircraft Applications (Fracture Toughness)

## Slide 19
resin impregnation
VARTM
resin
Vacuum pump
CNT coated fabric
Composition: CNT + Epoxy + Carbon fiber composite
Processing
Microstructure
Electrophoretic deposition
Uniform coating of CNT on fabrics
Processing of composites
Use CNT coated fabric now to make composite
Property
Increase in in-plane and out-of-plane electrical conductivity increased because of CNTs
Problem - Lightning
Property needed - Electrical conductivity
Materials Needs for Aircraft Applications (Lightning Strike)

## Slide 20
Problem - Icing
Property needed - Electrical & thermal conductivity
Composition: Graphene Oxide + Polyamide + Carbon fiber composite
Microstructure
Processing of composites
Significant improvements in thermal conductivity for composites with various chemical treatments
Property
Materials Needs for Aircraft Applications (Icing)

## Slide 21
resin impregnation
VARTM
resin
Vacuum pump
CNT coated fabric
Composition: CNT + Epoxy + Carbon fiber composite
Processing
Microstructure
Electrophoretic deposition
Uniform coating of CNT on fabrics
Processing of composites
Use CNT coated fabric now to make composite
Property
Internal damages which is not shown in load-displacement curves are shown as change in resistances – beneficial to detect and monitor defects in internal structures
Problem - Structural health monitoring
Property needed - Electrical conductivity
Materials Needs for Aircraft Applications (Health Monitoring)

## Slide 22
Composition: Polymer + Self healing capsules or fibers + Carbon fibers
Microstructures
Problem - Structural health monitoring
self healing
Smart materials
Materials Needs for Aircraft Applications (Self Healing)
Hollow fibers with uncured resin are used. Under cracking of fibers, resin comes out and reacts with catalyst outside. It cures and closes the cracks.

## Slide 23
Outcomes:
Gain knowledge on different materials used in aircraft structures.
Understand the importance of composition - processing – microstructure – property relations in certain aircraft material (polymer composites).
Thank You